

|  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | logo |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
| **\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_** |
| 1813 McCullough Blvd. 38801 ~ Post Office Box 1427 38802 ~ Tupelo, MS 38801 ~ Ph 1-800-737-8272 ~ Fax 662-844-8511 |
|  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **SECURITY SCREEN SPECIFICATIONS** |
|  | **#125 ECONOMY SERIES** |
|  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **A. Sub-Frame: Extruded aluminum 6063-T5, .062 wall thickness,**  |  |
|  |  **1.437" x 1.065 single hollow. Weight per ft .360** |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **B. Main Frame: Extruded aluminum 6063-T5, 1.390" Wide x .966" Height,** |
|  |  **.060 wall thickness. Weight per ft .340** |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **C. Corner Gussets: Shall be .250 solid aluminum or welded corners.**  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **D. Spreader Bar: Extruded aluminum 6063-T5, 1.00" x .400" with .060 wall** |
|  |  **thickness.** |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **E. Wire Mesh: Stainless steel with natural or painted finish or perforated** |
|  |  **with powder coat paint, .028 or .035 12 x 12 mesh.** |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **F. Anchor Bar: Extruded aluminum 6063-T5, 1.00" wide x .060 wall thickness.** |
|  |  **Screws not to exceed 4" apart.**  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **G. Hinge: Top or side pivot - 1/4" x 2-3/8" SST pivot rod.**  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  | **H. Latches: Stainless steel barrel bolt latches or optional single point** |  |
|  |  **release latch.** |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |
|  |  **I. Finish: Mill Finish, Bronze, White** |  |  |  |  |  |